NPRE 470 NOTES 2/03/2011

Fuel Combustion vs Nuclear Heating

- Reforming of methane and water to yield carbon monoxide and hydrogen gas, enthothermic

- Further carrying on the reaction is the water gas shift that converts carbon monoxide and water to carbon dioxide and hydrogen gas, exothermic

- When nuclear heating is used in the above process yield is increased by 30% compared to fuel heating

Purification of Hydrogen Gas

- Use of pressure swing adsorption (PSA) which differentiates between carbon monoxide and hydrogen gas based on their masses and Van der Waals force

- Since carbon monoxide has dipoles on both oxygens it can stick to an ionized wall

- The PSA has alumina on the bottom, followed by carbon black, and finally zeolite on top that are used to trap different size molecules

- For PSA’s the feed gas comes in at constant flow, and constant high pressure.  The hydrogen comes off the top at a high purity (>99.9 vol%) with constant flow and constant high pressure.  The carbon monoxide and off gasses come off the bottom with constant flow, constant low pressure, and constant concentration

PSA Advantages/Disadvantages

- Adv: Simple mechanism

- Dadv: batch type operations

Membrane Separators

- Usually a Pd based alloy

- Separates the hydrogen molecule into atoms and recombines them after the atoms have passed through the membrane

- In general they are tube-like structure to better withstand pressure

- Can use one membrane reactore in place of steam reformer, water gas shift, and PSA